Table 1. Single crystal XRD data of 4MB crystal

| Unit cell dimensions |  | a = 14.4691(10) A alpha = 90 deg. |
| --- | --- | --- |
|  |  | b = 14.0978(10) A beta = 90 deg. |
|  |  | c = 5.8468(4) A gamma = 90 deg. |
| Volume |  | 1192.64(14) Å3 |
| Z, Calculated density |  | 4, 1.349 mg/m3 |
| Crystal system, space group |  | Orthorhombic, Pca21 |
| Refinement method |  | Full-matrix least-squares on F^2 |